📄 GitHub README

# Reaction Energy Data for Gr/Si (111) Catalysis (Fig. 6)

This repository provides the quantitative reaction energetics underlying Fig. 6 of the manuscript:

The dataset contains Density Functional Theory (DFT) reaction energies and activation barriers for gas activation on pristine and defected Gr/Si interfaces. These data support the mechanistic interpretation presented in the main text.

## Overview

The calculations compare the catalytic behavior of pristine vs defected graphene/silicon interfaces for three representative molecules:

- H2S

- SO2

- N2O

The data include:

- Reaction energies (ΔE)

- Activation barriers (Ea)

- Experimental benchmarks where available

All values are extracted directly from the manuscript and Supporting Information.

## Data Summary

| Molecule | Surface (Gr/Si) | E ads* (kJ/mol) | ΔE reaction (kJ/mol) | Ea (DFT) (kJ/mol) | Experiment Ea (kJ/mol) |
| --- | --- | --- | --- | --- | --- |
| H₂S | Pristine | -25.1 | +118 | 112 | No dissociation |
| H₂S | Defected | -36.6 | -102 | 29 | 23 |
| SO₂ | Pristine | -48.4 | +148 | 162 | No dissociation |
| SO₂ | Defected | -63 | -2.2 | 67 | 52.8 |
| N₂O | Pristine | -48 | -126 | 202 | No dissociation |
| N₂O | Defected | -76 | -401 | 190 | No dissociation |
| *Experimental Ead of H2S, SO2, and N2O on the whole sample, including both pristine and defected parts, are -27.4, -46.2 and -33.3 kJ/mol, respectively. |  |  |  |  |  |

## Methodology (Brief)

- Electronic structure calculations: Density Functional Theory (DFT)

- Transition states: CI-NEB where applicable

- Additional validation has been done via finite-temperature simulations. Full computational details are provided in the manuscript Supporting Information.

## Interpretation

The data demonstrate a clear defect-driven catalytic switch:

- Grain-boundary defects invert H2S reaction energetics from endergonic to strongly exergonic.

- SO2 follows a similar but weaker defect-mediated activation pathway.

- N2O remains kinetically hindered despite favorable thermodynamics due to a large activation barrier.

The dataset reflects the defect-dependent trends discussed in Fig. 6.